## Slide 1: Air barrier requirements

## Slide 2: Energy Code - Air Barrier Requirements
Material air permeability ≤ 0.004 cfm/ft2 per ASTM E2178 (IECC 2012 C402.4.1.2.1)
Some codes may list “deemed-to-comply” air barrier materials
  Best to verify with product manufacturer’s test data
Typical types of air-barrier materials or assemblies
  Sheathing (gypsum board, FPIS, WSP, etc.)
  Concrete / stucco / parged (mortar finished) masonry
  Membranes (wraps, spray/elastomeric, peel-and-stick, etc.)
Notes: While air-barriers are found in the energy code because they help stop energy loss due to whole building air-leakage, they are also important to the moisture control provisions in the building code. For example, vapor retarders can stop moisture vapor diffusion only if there is also a continuous well-sealed air-barrier to prevent moisture from moving into an assembly by air-movement. For some conditions, far more moisture can be moved into a building assembly by air-leakage than by vapor diffusion through a vapor retarder.

## Slide 3: Air Barrier Applications of FPIS
Many FPIS products are AB materials
  Refer to TER No. 1410-06
  As with any air-barrier material, the installed performance depends on good joint sealing
Notes: Most foam sheathing products meet air-barrier, or AB, material requirements that are based on air permeability tests.
For a specific product, check with the manufacturer.
ABAA provides guidance on air barrier requirements. “An air barrier material is any building material that has a air leakage rate that is not greater than 0.02 L/(s•m2) @ a pressure differential of 75Pa (0.004 cfm/ft2 at a pressure differential of 1.57 lb/ft2).”
To create a good air barrier, it’s key to properly seal the joints.
An ideal approach is to have a dual air-barrier on both the inside and outside of a wall, but the code only requires a barrier on one side. Ensure that the air barrier on one side of the wall is vapor permeable to allow drying of the wall where incidental moisture occurs within the cavity.
http://www.buildingscience.com/documents/digests/bsd-106-understanding-vapor-barriers

## Slide 4: Air Barrier Applications of FPIS
AB application tips:
  Though code requires AB only on one side of wall, both sides will give better thermal and moisture control
  Know the difference between AB and vapor barrier
    An air barrier stops the movement of air into or out of the conditioned space
    A vapor barrier slows or reduces the movement of water vapor through a material.
  Like other materials, air-barriers have vapor permeance properties and should be coordinated with the code-compliant vapor control strategy for a wall assembly.
Notes: Most foam sheathing products meet air-barrier, or AB, material requirements that are based on air permeability tests.
For a specific product, check with the manufacturer.
ABAA provides guidance on air barrier requirements. “An air barrier material is any building material that has a air leakage rate that is not greater than 0.02 L/(s•m2) @ a pressure differential of 75Pa (0.004 cfm/ft2 at a pressure differential of 1.57 lb/ft2).”
To create a good air barrier, it’s key to properly seal the joints.
An ideal approach is to have a dual air-barrier on both the inside and outside of a wall, but the code only requires a barrier on one side.